|  | STANDARD OPERATING PROCEDURE | Document ID:JODL/PB PT/03 |
| --- | --- | --- |
|  |  | Version: 1 |
|  | Slit Coil Inspection | Date: 01/01/2026 |

Purpose:

To inspect and verify the

for the production of Pipes & Tubes against the purchase order

Scope:

Each incoming coil

Teams and Responsibilities:

| Sl No | Team | Responsibility |
| --- | --- | --- |
| 1 | Contract Manufacturer | - Ensure size wise, grade wise and heat wise storage of incoming coils under covered shed - Provide all necessary resources to perform joint inspection - Carry out joint inspection with JSW One quality team - Provide designated space for rejected coils - Intimate supplier in case of any non-compliance |
| 2 | SGS QC Engineers | - Joint Inspection of incoming coils along with contract manufacturer, - Ensure all rejected coils are quarantined and suitably identified - Prepare joint inspection report |
| 3 | JSW One Operation/Quality Manager | - Decision making on acceptance as and when required - Maintain laid out inspection process as described in this SOP |

Standard Operating Process:

- After the slitting and recoiling are complete, the 100% slit coils to be inspected before packaging and pipe manufacturing.

- Measure the final width of the slit coil and check whether width matches with planned width.

- Inspect the slit edges for burrs, knife marks, or rough fractures.

- Evaluate the finished coil for shape defects like excessive camber or a "crossbow" curvature.

- Inspect the surface for mechanical damage, abrasion mark or any other surface imperfection that may occur during slitting process

- Check that the coils are tightly wound and properly strapped to prevent damage during storage and transportation to pipe forming units.

- Verify whether coils are weighed after slitting process.

- Check the label/identification to ensure full traceability

- Take following actions in case of any deviation or non-compliance :

- In case of absence of identification and traceability in any of the coil, hold the coil for processing and inform Contract Manufacturer. After verification of all required properties (such as chemistry, mechanical properties, dimension) decision to use the coil(s) shall be taken.

- In case of presence of surface defects, coil(s) to be rejected, quarantined and identified by RED tag or any other suitable method.

- In case, width does not conform to the planned width, coils to be kept on hold. Based on requirement, such coils may be diverted for alternative pipe sizes after discussion.

Records

- Slit Coil Joint Inspection Report as per QF No. JSW One/PT/ICJTR/02

- Slit Coil Joint Inspection Report to be duly signed by SGS QC Engineer and Contract Manufacturer representative

| JSW One Quality Head | Contract Manufacturer |
| --- | --- |