|  | STANDARD OPERATING PROCEDURE | Document ID:JODL/PB PT/08 |
| --- | --- | --- |
|  |  | Version: 1 |
|  | Joint Inspection of Tensile Properties of Pipes & Tubes | Date: 01/01/2026 |

1.0 Purpose:

To check and report the mechanical properties (Yield Strength, Ultimate Tensile Strength, %Elongation) of Pipes & Tubes jointly with Contract Manufacturer team

2.0 Scope:

Pipes and Tubes final product

3.0 Applicable standard:

- IS 4923, IS 1161,IS 3601 for acceptance and sampling

- IS 1608 for procedure

- IS 4711 for sampling

4.0 Teams and Responsibilities:

| Sl No | Team | Responsibility |
| --- | --- | --- |
| 1 | Contract Manufacturer-Chemist | Testing of Tensile properties of Pipes & Tubes samples |
| 2 | SGS QC Engineers | - Ensure test process as per IS 1608 - Witness test, verify test results w.r.t acceptance criterion and clearance - Preparation of Joint Inspection Report |
| 3 | JSW One Quality Manager | Ensure the accepted Tensile properties are as per JSW One product standard and applicable BIS requirements for final clearance and approval |

- Pre-testing Verifications:

  - Calibration status of concerned Universal Testing Machine to be verified by SGS QC Engineers before joint inspection.

  - If the instrument is out of calibration or calibrated by non-NABL agency, the concerned Universal Testing Machine shall not be used for testing

- Sampling Plan.

As per applicable BIS standard

- Test Piece Preparation

- Location: Extract the test piece from the section excluding the side where the weld seam is located.

- Shape: Samples are typically strips cut longitudinally or full-section specimens for smaller diameters.

- Gauge Length: The elongation percentage must be measured on a proportional gauge length calculated as: 
Lo=5.65√So ,

So is the original cross-sectional area of the test piece.

- Test Procedure:

- Follow test method as described in IS 1608 standard

- Measurement: Measure the original dimensions (width and thickness) to calculate the cross-sectional area S0

- Marking: Mark the gauge length L0 on the specimen

- Mounting: Secure the specimen in the grips of a Universal Testing Machine (UTM).

- Loading: Apply a continuous tensile load until the specimen fractures.

- Observation: Monitor the load to identify the Yield Point and the maximum load for Ultimate Tensile Strength (UTS).

- Final Measurement: Fit the fractured ends together to measure the final gauge length (Lu) to determine elongation.

8. Acceptance Criterion:

Grade wise specification as per IS 4923/IS 1161/IS 3601 for tensile properties are given in the below Table:

| Grade | Yield Strength (Min) | Tensile Strength (Min) | Elongation (Min %) |
| --- | --- | --- | --- |
| YSt 210 | 210 MPa | 330 MPa | 20% for sizes >25.4mm 12% for size≤25.4mm |
| YSt 240 | 240 MPa | 410 MPa | 15% for sizes >25.4mm 10% for size≤25.4mm |
| YSt 310 | 310 MPa | 450 MPa | 10% for sizes >25.4mm 8% for size≤25.4mm |

The pipe is considered to be compliant if the yield strength, tensile strength, and elongation meet or exceed the values specified for its grade in the table above.

If any test fails, two samples for concerned batch to be collected and tested. If both the samples pass, then only the batch to be accepted.

9.0 Records:

Duly signed Joint Inspection Report by Contract Manufacturer and SGS QC Engineer

| JSW One Quality Head | Contract Manufacturer |
| --- | --- |