|  | STANDARD OPERATING PROCEDURE | Document ID:JODL/PB PT/01 |
| --- | --- | --- |
|  |  | Version: 1.0 |
|  | Incoming Coil Inspection | Date: 01/01/2026 |

Purpose:

To inspect and verify the incoming coil quality for the production of Pipes & Tubes against the purchase order

Scope:

Each incoming coil

Teams and Responsibilities:

| Sl No | Team | Responsibility |
| --- | --- | --- |
| 1 | Contract Manufacturer | - Ensure size wise, grade wise and heat wise storage of incoming coils under covered shed - Provide all necessary resources to perform joint inspection - Carry out joint inspection with JSW One quality team - Provide designated space for rejected coils - Intimate supplier in case of any non-compliance |
| 2 | SGS QC Engineers | - Joint Inspection of incoming coils along with contract manufacturer, - Ensure all rejected coils are quarantined and suitably identified - Prepare joint inspection report |
| 3 | JSW One Operation/Quality Manager | - Decision making on acceptance as and when required - Maintain laid out inspection process as described in this SOP |

Standard Operating Process:

- Check MTC of the incoming batch and verify whether chemistry and mechanical properties of the batch comply with the applicable BIS requirements.

- Check whether identification markings-supplier name, size, grade, heat/cast number are present in each coil.

- Verify weight of each coil against the quantity mentioned in the invoice and MTC.

- Check the thickness of the coil by micrometer/Vernier calipers.

- Check the width of the coil by measuring tape.

- Visually inspect 100% coils to check presence of any harmful surface defects such as seams, folds, cracks, pits, excessive scaling, rust spots, waviness, kinks, twist, camber, distortion, center buckle, wavy edge.(Please refer Annexure A)

- Take following actions in case of any deviation or non-compliance :

- In case of absence of identification and traceability of any of the incoming coil, hold the coil for processing and inform Contract Manufacturer and Coil Supplier. After discussion with Supplier and verification of all required properties (such as chemistry, mechanical properties) decision to use the coil(s) shall be taken.

- In case of any mismatch of actual grade and size against PO, entire batch to be rejected for intended use or to be diverted for alternative use after a mutual decision between Contract Manufacturer and JSW One team.

- In case of presence of surface defects, coil(s) to be rejected, quarantined and identified by RED tag or any other suitable method.

- In case thickness is beyond the applicable BIS norm, reject the coil for the intended use or divert to other applicable if comply with the alternative BIS standard.

- In case of any deviation in width against the planned width, intimate the Contract Manufacturer and JSW One Operation In-charge for decision

Records

- Incoming Coil Joint Inspection Report as per QF No. JSW One/PB PT/JTR/01

- Incoming Coil Joint Inspection Report to be duly signed by SGS QC Engineer and Contract Manufacturer representative

| JSW One Quality Head | Contract Manufacturer |
| --- | --- |