|  | STANDARD OPERATING PROCEDURE | Document ID:JODL/PB PT/03 |
| --- | --- | --- |
|  |  | Version: 1.0 |
|  | Pipe and Tube Product Inspection | Date: 01/01/2026 |

Purpose:

To inspect Pipes & Tubes as per applicable BIS standards-IS 4923, IS 1161 and IS 3601 and JSW One Product Standard

Scope:

Pipes and Tube products in black and galvanized condition during and after production as applicable

Applicable Standard:

- Latest versions of IS 4923, IS 1161 and IS 3601

- JSW One Product Standard

Teams and Responsibilities:

| Sl No | Team | Responsibility |
| --- | --- | --- |
| 1 | Contract Manufacturer | - Provide all necessary resources to perform joint inspection - Carry out joint inspection with JSW One quality team - Provide designated space for prime and rejected products - Take immediate correction and initiate corrective action in case of deviation during in-process inspection and testing |
| 2 | SGS QC Engineers | - Joint Inspection and testing of pipes and tube along with contract manufacturer - Immediate intimation to Contract Manufacturer in case of deviation - Segregation of rejected product with suitable marking - Prepare joint inspection report |
| 3 | Dispatch Executive | - Pre-Dispatch Inspection |
| 3 | JSW One Operation/Quality Manager | - Decision making on acceptance as and when required - Maintain laid out inspection process as described in this SOP |

Pre-inspection Verification:

- Check whether all testing equipment and instruments are calibrated

- If any of the instrument or equipment is out of calibration or calibrated by non-NABL agency, the concerned testing facility shall not be used for testing and inspection process

- QC Inspector of Contract Manufacturer and JSW One must be available at the time of production

Safety Protocol:

- All QC inspectors from both the parties must wear necessary Personal Protective Equipment- Helmet, Safety Shoes, Goggles, Ear Plug during in-process and offline inspection

Standard Operating Process:

- SGS QC Engineer and QC Inspector of Contract Manufacturer shall be present during the production of tubes.

- After the completion of job setting process, Contract Manufacturer team shall intimate start of prime production to SGS QC Engineer.

- Testing shall be carried out as per applicable BIS standard as given in Table 1.

- Testing activities shall be performed jointly by Contract Manufacturer QC Inspector and SGS QC Engineer. All the test result must be mutually agreed by Contract Manufacturer QC inspector and SGS QC Engineer.

- After the start of prime production, samples shall be collected by SGS QC Engineer to check dimensional, chemical and mechanical properties as per the frequency defined in Table 2.

Table 1: Test Plan

| Sr. No | Type of Test | Property | Applicable Standard |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | IS 1161 | IS 4923 | IS 3601 |
| 1 | Tensile Testing | Yield Strength | √ | √ | √ |
|  |  | Ultimate Tensile Strength | √ | √ | √ |
|  |  | %Elongation | √ | √ | √ |
| 2 | Chemical Testing | Chemistry | √ | √ | √ |
| 3 | Ductility Testing | Cold bend test | √ | X | √ |
|  |  | Flattening Test | √ | X | √ |
|  |  | Drift Expansion Test | X | X | √ |
|  |  | Crushing Test | X | X | √ |
| 4 | Dimension Check | Straightness | √ | √ | √ |
|  |  | Length | √ | √ | √ |
|  |  | Thickness | √ | √ | √ |
|  |  | Outer Diameter | √ | X | √ |
|  |  | Ovality | √ | X | √ |
|  |  | Inside weld height | √ | √ | √ |
|  |  | Outer side | X | √ | X |
|  |  | Squareness | X | √ | X |
|  |  | Radii of corned | X | √ | X |
| 5 | Weight check | Weight/m | √ | √ | √ |
| 6 | Visual Check | Surface finish, end finish | √ | √ | √ |

Table 2: Sampling Plan

| Sr. No. | Parameter | Sampling Frequency | Test Standard | Remark |
| --- | --- | --- | --- | --- |
| 1 | Chemistry | 1 Sample/heat | IS 228 | In absence of chemical test facility, MTC for corresponding heat can be referred |
| 2 | Outer dimension, Squareness, Radii of curvature | One sample/hour of production | - | In-process sample |
| 3 | Thickness | One sample/hour of production | - | In process sample |
| 4 | Length | 1 sample/hour of production | - | In process sample |
| 5 | Tensile Test | 1 coil/heat and 1 sample/4 hour of production | IS 1608 | In process sample |
| 6 | Straightness | Each pipe | - | After production |
| 7 | Visual Inspection of surface quality | Each pipe | JSW One Visual Inspection standard | In process and after production |
| 8 | Cold bend test | 1 sample/hour of production | IS 2329 | In process sample |
| 9 | Flattening test | 1 sample/hour of production | IS 2328 | In process sample |
| 10 | Weight/m | 1 sample/hour of production | - | In process sample |

- Acceptance criterion shall be as per the JSW One product standard and applicable BIS specification

- If any deviation from acceptance criterion observed during in-process inspection, immediately concerned production in-charge of the Contract Manufacturer shall be informed and rolling shall be stopped till action taken to eliminate the defect/deviation and effectiveness of the action is evidenced.

- In case of any deviation from the acceptance norms, pipes produced during the time period shall be identified, quarantined and labelled as ‘hold’ or ‘reject’ depending on the type of nonconformity.

- In case of materials under ‘hold’, two additional samples to be collected from the concerned lot. If both these samples pass the test, the lot shall be accepted and even if one sample fails to pass, lot shall be rejected.

- The rejected lot shall be segregated and quarantined at a designated location and identified by red label/red paint or other suitable method mutually agreed between JSW One and Contract Manufacturer.

- Investigation of root cause shall be carried out jointly by the Contract Manufacturing and JSW One Quality Team and submit the investigation report with corrective action within 2 working days.

- All accepted materials shall be stored at a location designated for prime materials.

- All prime pipes which are ready to dispatch shall be fully traceable and marked as per applicable product standard and JSW One norm.

- Presence of identification and traceability in the final pipe shall be checked before dispatch.

- All prime pipes shall be bundled as per JSW One SOP and the status of the bundling shall be checked before dispatch.

- Consolidated test results shall be recorded in a Joint Inspection Report (JTR). JTR shall be duly signed by Contract Manufacturer QC Inspector and SGS QC Engineer.

- Only acceptable lots shall be considered for dispatch.

- During dispatch, pre-dispatch inspection (PDI) shall be carried out by the dispatch executive as per JSW One PDI format for each consignment.

- PDI report shall be duly signed by Dispatch Executive

- In case of any mismatch from the Delivery Order and actual loaded materials, consignment shall be hold till the action is taken.

- Test results of the acceptable lots shall be reported in the Material Test Certificate.

Record:

- Duly signed Joint Inspection Report

- Pre dispatch inspection report

- Daily Quality Report

| JSW One Quality Head | Contract Manufacturer |
| --- | --- |