|  | STANDARD OPERATING PROCEDURE | Document ID:JODL/PB PT/07 |
| --- | --- | --- |
|  |  | Version: 1.0 |
|  | Joint Inspection of Bend Test of Pipes & Tubes | Date: 01/01/2026 |

1.0 Purpose:

To assess the Bendability of Pipes & Tubes

2.0 Scope:

Circular Hollow Section Pipes and Tube Products up to 50mm nominal bore size

3.0 Applicable Standards:

- IS 1161, IS 3601 for acceptance standard

- IS 2329: Method for bend test (General standard for bend testing)

- IS 4711: Procedure for sampling of tubes

4.0 Teams and Responsibilities:

| Sl No | Team | Responsibility |
| --- | --- | --- |
| 1 | Contract Manufacturer | - Ensure availability and proper condition of bend testing machines at the time of testing - Joint testing of Bendability |
| 2 | SGS QC Engineers | - Joint testing of Bendability - Preparation of Joint Inspection Report |
| 3 | JSW One Operation/Quality Manager | Ensure the bendability is checked for all lots and acceptable as per applicable BIS standard |

- Equipment:

- Bend testing machine ( Bending machine or a universal testing machine with appropriate fixtures)

- Former (Mandrel): Formers with a specific radius for bending as per dimension

- Cutting tools: For obtaining test samples.

- Measuring instruments: Vernier Caliper, measuring tape.

6.0 Test Procedure

- Sampling Frequency: One sample shall be drawn for each size of pipe per hour of production with a minimum one sample per heat/size as per sampling plan outlined in IS 4711.

- Sample Size: A representative length of pipe is cut for testing.

- Weld Placement: The test specimen must be oriented so that the weld is positioned at the outermost part of the bend (at an angle of 90° to the plane of bending).

- Surface Preparation: The ends of the sample should be free from sharp edges and burrs. Galvanized coatings may be removed before testing, if necessary, although the standard also outlines criteria for galvanized tubes.

- Test Execution

- The test can be carried out on the full pipe section.

- For Non-galvanized (Black) Tubes: The test piece is bent cold through 180 degrees around a former.

- For Galvanized Tubes: The test piece is bent cold through 90 degrees around a former.

- The radius of the former (at the bottom of the groove in the place of bending) must be as follows:

- Non-galvanized Tubes: The radius should be at least six times the outside diameter of the tube (6D).

- Galvanized Tubes: The radius should be at least eight times the outside diameter of the tube (8D).

7.0 Inspection and Acceptance Criteria

- Visual Inspection: After bending, the sample shall be inspected visually for any signs of fracture, cracks, or failure at the weld and the metallic area.

- Acceptance Criterion: The pipe material is deemed to pass the test if no cracks or fractures occur at the weld or the metal.

8.0 Re-testing Procedure

- If the initial test piece fails, two further samples from the same batch shall be selected and tested in respect of the failure.

- If both additional samples pass, the material batch is considered compliant with the standard.

- If either of the additional samples fails, the entire batch represented by the samples is considered non-compliant with the standard.

9.0 Records

Duly signed Joint Inspection Report for bend test by Contract Manufacturer and SGS QC Engineer

| JSW One Quality Head | Contract Manufacturer |
| --- | --- |