|  | STANDARD OPERATING PROCEDURE | Document ID:JODL/PB PT/08 |
| --- | --- | --- |
|  |  | Version: 1.0 |
|  | Joint Inspection of Flattening Test of Pipes & Tubes | Date: 01/01/2026 |

1.0 Purpose:

To assess the ductility and soundness of weld metal and parent metal of Pipes & Tubes

2.0 Scope:

Circular Hollow Section Pipes and Tube Products above 50mm nominal bore size

3.0 Applicable Standards:

- IS 1161, IS 3601 for acceptance standard

- IS 2329: Method for bend test (General standard for bend testing)

- IS 4711: Procedure for sampling of tubes

4.0 Teams and Responsibilities:

| Sl No | Team | Responsibility |
| --- | --- | --- |
| 1 | Contract Manufacturer | - Ensure availability and proper condition of bend testing machines at the time of testing - Joint Flattening Test |
| 2 | SGS QC Engineers | - Joint Flattening Test - Preparation of Joint Inspection Report |
| 3 | JSW One Operation/Quality Manager | Ensure Flattening Test is performed for all lots and acceptable as per applicable BIS standard |

5.0 Test Procedure

- A ring specimen is cut from the end of a finished tube.

- The length of the sample is usually not less than 40 mm (often 50-100 mm range).

- The edges of the specimen may be rounded or chamfered by filing or other methods to prevent premature edge cracking.

- A universal testing machine or press with parallel plates is used. The width of the plates must exceed the width of the flattened sample.

- The weld seam must be placed at 90° or 180° to the direction of the applied force (maximum bending points).

- The specimen is placed between the parallel plates and compressed in a cold state (room temperature) at a speed not exceeding 50 mm/min.

- The test continues until the distance between the plates reaches a specific value relative to the original outside diameter as per the relevant BIS standard

6.0. Acceptance Criteria:

No opening/crack in the weld until the distance between plates is less than 75% of the original outside diameter.

Metal (Elsewhere): No cracks or breaks in the metal (other than the weld) until the distance between plates is less than 60% of the original outside diameter.

7.0 Retest:

If a specimen fails, two additional samples should be selected from the same lot for retesting. If both pass, the lot is accepted; otherwise, the lot is rejected.

8.0 Records

Duly signed Joint Inspection Report for bend test by Contract Manufacturer and SGS QC Engineer

| JSW One Quality Head | Contract Manufacturer |
| --- | --- |