|  | STANDARD OPERATING PROCEDURE | Document ID:JODL/PB PT/JT/09 |
| --- | --- | --- |
|  |  | Version: 1.0 |
|  | Joint Inspection of Dimensional characteristics of Pipes & Tubes | Date: 01/01/2026 |

1.0 Purpose:

To assess the dimensional parameters of Pipes and Tubes

2.0 Scope:

Square and Rectangular Hollow Section

3.0 Applicable Standards:

- IS 4923, IS 1161, IS 3601

- IS 4711: Sampling Frequency

4.0 Teams and Responsibilities:

| Sl. No | Team | Responsibility |
| --- | --- | --- |
| 1 | Contract Manufacturer | - Provide measuring instruments as necessary - Joint inspection of dimensional characteristics |
| 2 | SGS QC Engineers | - Joint inspection of dimensional characteristics - Preparation of Joint Inspection Report |
| 3 | JSW One Operation/ Quality Manager | Ensure dimensional characteristics are compliant to IS 4923 requirements |

5.0 Sampling

One sample per hour of production with a minimum of one sample per heat/size

6.1 Twist Measurement:

- Twist is the maximum longitudinal deviation of the corners along the length of the section as depicted in Figure 1.

Figure 1: Twist

- Place the hollow section on a flat horizontal surface (e.g., a calibrated surface table or flat rails).

- Ensure one side of the hollow section at one end is pressed flat against the horizontal surface.

- At the opposite end of the hollow section, measure the vertical distance (V) between the surface table and the lowest corner of the section that is lifted off the table as per Figure 1 by using Precision Ruler-Vernier Caliper Feeler Gauge-Micrometer for higher accuracy.

- The measurements are taken from the outer, rounded corners of the hollow section.

- The twist to be measured cold forming and cutting to length.

- The measured vertical distance is represented as Total Twist in mm.

- If the section is very long, the twist can be measured relative to the distance between the corners, as defined by the standard.

6.2. Squareness of corner measurement:

- Squareness of the corner for a Rectangular Hollow Section (RHS) or Square Hollow Section (SHS) refers to the deviation of the angle between adjacent sides from a perfect 90°

- Before the measurement, clean the RHS/SHS and remove any burrs or weld spatter from the corner being tested.

- Take measurements at least 50mm (or 2 inches) from the end of the section, as distortion often occurs at the cut ends.

- Use a digital protractor to measure the angle directly, ensuring the tool is not affected by convexity or concavity.

- Repeat the procedure for all four corners and for both the ends.

6.3. Radii of corner measurement:

- Maximum allowable corner radii is measured to ensure structural integrity of the pipes.

- Identify where the flat side of the hollow pipe ends and the corner curve begins (the tangent point).

- Place a straight edge tool along one flat side of the corner to be measured.

- Place the ruler perpendicular to the straight edge, touching the start of the corner curve on the adjacent side.

- The distance from the start of the curve to the perpendicular straight edge represents the corner radius.

- Measure all four corners and both the ends.

- Alternatively if an internal radius gauge is available, it can be inserted into the corner to get a direct reading.

6.4. Convexity/Concavity Measurement:

- Concavity or convexity (deviation from flat sides) of square or rectangular hollow sections (SHS/RHS) is checked by measuring the maximum deflection of the side face from a straight line connecting the corners.

- A straight edge (steel rule or specialized caliper) is placed across the face of the pipe, parallel to the sides, at the center of the cross-section.

- Place the straight edge across one flat side (width B or height H) of the section.

- Measure the maximum gap or deflection-x1 for concavity and x2 for convexity as per the below figure 2 between the straight edge and the surface of the hollow section.

Fig 2: Concavity/Convexity measurement

The percentage concavity or convexity is calculated as:

Maximum Measured Deviation Width or Height of the side X 100%

  - Straightness Check

- Place spacer blocks of equal height at both ends of the pipe or place the pipe on a flat and stable surface

- Stretch a thin, strong, non-stretchable wire tightly between the two spacer blocks or between two ends of the pipe along the concave side of the pipe.

- Locate the point of maximum deviation (the greatest distance between the wire and the pipe surface).

- Measure the maximum chord height (deviation) in millimeters using a ruler or feeler gauge.

- Calculation:

Maximum Measured Deviation(mm) Total Length of pipe(mm)

- End Straightness (End Hooking) Check

Check specifically for "end hooking" (bends near the ends) by applying the straight edge/wire at the last 1–2 meters of the pipe and use the above calculation.

7.0 Acceptance Criterion:

| Dimensional Characteristic | Acceptance Criterion | Reference Standard | Remark |
| --- | --- | --- | --- |
| Twist | 2mm+0.5mm/mm | IS 4923 | In case of deviation, reject the lot |
| Squareness of corner | 90˚±2˚ | IS 4923 |  |
| Radii of corner | 3Xthickness max | IS 4923 |  |
| Concavity/Convexity | 1% of size | IS 4923 |  |
| Straightness | 1/600th mm for machine straightened pipe | IS 4923, IS 1161, IS 3601 | Re-straighten in case of deviation |

8.0 Sampling Plan:

1 sample per hour of production

9.0 Record

- Duly signed Joint Inspection Report by Contract Manufacturer and SGS QC Engineer.

| JSW One Quality Head | Contract Manufacturer |
| --- | --- |