|  | STANDARD OPERATING PROCEDURE | Document ID:JODL/PB PT/JT/15 |
| --- | --- | --- |
|  |  | Version: 1.0 |
|  | Handling of nonconforming Pipes and Tube products | Date: 01/01/2026 |

Purpose:

Identification, segregation and disposition of the nonconforming Pipes and Tube products

Scope:

Pipes and Tubes

Teams and Responsibilities:

| Sl No | Team | Responsibility |
| --- | --- | --- |
| 1 | Contract Manufacturer | Identification and segregation of the nonconforming materials at designated locations |
| 2 | SGS QC Engineers | Ensure proper identification and segregation of nonconforming material at designated locations |
| 3 | JSW One Operation Manager | Ensure no mix-up of rejected material with prime material and 100% cutting and scrapping of the rejected pipes |

- Standard Operating Process:

- Following material shall be classified as nonconformity as given in the below Table:

| Type of nonconformity | Criterion for rejection | Disposition Action |
| --- | --- | --- |
| Non-compliance with Mechanical properties | IS 4923, IS 1161, IS 3601 | Reject |
| Non-compliance with Chemistry requirement | IS 10748 | Reject |
| Non-compliance for Surface defects | -Improper weld(open weld, Overlap, Butt weld) - Presence of rolling line, deep scratch, crack, inclusion or any other surface defects | Reject |
| Non-compliance to length | Customer requirement |  |
|  | IS 4923, IS 1161, IS 3601 |  |
| Non-compliance to straightness | IS 4923, IS 1161, IS 3601 | Hold till the lot is re-straightened and passed. If fails after re-straightening, Reject |
| Non-compliance to weight/m | IS 4923, IS 1161, IS 3601 | Reject |
| Non-compliance to bend and flattening test | IS 1161, IS 3601 | Reject |
| Non-compliance to dimensional parameters | IS 4923, IS 1161, IS 3601 | Reject |
| Non-compliance to Drift Expansion Test | IS 3601 | Reject |
| Non-compliance to Crushing Test | IS 3601 | Reject |

- All rejected lot shall be segregated and identified with RED paint/or two RED labels per bundle

- Rejected lots shall be kept at a separate designated ‘Rejection Area’ and the place must be far from prime product locations.

- All rejected pipes shall be cut into 3-4 pieces within 7 days of generation and cu pieces shall be scrapped.

- JSW One Operation Manager/SGS QC Engineers shall check the status of identification of the rejected pipes on daily basis and monitor the cutting of the pieces periodically.

- If the cutting of the rejected pipes are not being done within 7 days, JSW One

team shall intimate the Contract Manufacturer.

- Records:

Internal rejection report

| JSW One Quality Head | Contract Manufacturer |
| --- | --- |